## Slide 1
AF2903 Road Construction and Maintenance
Compaction of Hot Mix Asphalt
Dr. Alvaro Guarin
Highway and Railway Engineering Department of Transportation Science

## Slide 2: Compaction of Soils/Granular Materials

## Slide 3: Compaction of Asphalt Mixtures
To Minimize Additional Compaction
To Minimize Permeability
To Prevent Excessive Oxidation of the Asphalt Mixture
To Provide Adequate Shear Strength
Three Phases of Rolling
Breakdown Rolling
Intermediate Rolling
Finish Rolling

## Slide 4: Breakdown Rolling
Vibratory Steel Wheel Roller (Mostly)
Rubber Tired Roller (Sometimes / Tender mixes)
Static Steel Wheel Roller (Rarely)
Three Wheel Roller (not desired)
Generally induces the most density gain of any roller in the sequence. Breakdown rollers can be of any type but are most often vibratory steel wheel and sometimes pneumatic tire.

## Slide 5: Intermediate Rolling
Provides additional compaction.
Rubber Tired Roller (Kneading action)
Vibratory Steel Wheel Roller
Finish Rolling
Offers a smooth mat surface.
Static Steel Wheel Roller

## Slide 6: Breakdown Roller
Should Stay Immediately Behind the Paver

## Slide 7
Vibratory Steel Wheel Roller

## Slide 8
Rubber Tired Roller
Right after breakdown compaction

## Slide 9: Heaters for the Tires

## Slide 10: Skirts Around Rubber Tires

## Slide 11
Planning the Compaction Sequence
What is the time window for compaction? (depends on temperature of mix, air, ground, weather, wind, etc)
How many rollers, how many passes?
Rolling patterns

## Slide 12
Type of compaction equipment
Paving width
Roller width
Number of passes
Roller speed
Number of rollers
Roller pattern depends on:

## Slide 13
Roller Speed
Rollers Should Operate at a Slow Rate of Speed (about Walking Speed).

## Slide 14
Roller Speed
Not too slow…
Not too fast…

## Slide 15
Roller Pattern
Rollers Should Avoid Sudden Stops, Starts, or Turns

## Slide 16
Intelligent Compaction
The precise location of the roller, its speed, and number of passes over a given location are mapped using the Global Positioning System (GPS) or a similar system.
To determine the effectiveness of the compaction process, compaction meters are mounted in or about the drum to monitor applied compaction effort, frequency, and response from the material being compacted.

## Slide 17
Instable mixture
Stiff mixture
Rolling behavior of HMA

## Slide 18
Compaction Temperature

## Slide 19: The Longitudinal Joint is Often the Biggest Problem Area
Longitudinal Joint

## Slide 20: Cutting Wheel has Been a Very Effective Method to Obtain Density at Longitudinal Joint
Notched wedge joint
Cutting wheel
Joint maker
Edge restraining device
Joint Construction Devices

## Slide 21
Notched Wedge Joint

## Slide 22
Cutting wheel

## Slide 23
Joint maker

## Slide 24
Edge restraining device

## Slide 25: Rolling joints
Transverse joints
Longitudinal joints
Cold mix
Hot mix
Hot mix
Cold mix
Joint Adhesion:
Heat the cold side before placing the hot side.
Coat the cold side with an adhesive material.

## Slide 26: Eliminate Longitudinal Joint
Use paver extension

## Slide 27: Echelon Paving

## Slide 28: Two Ways to Check Density
Cores
Insitu Measurements

## Slide 29
Scuffing of mix in front of the drum
Mix sticking to the drums
Asphalt Compaction Problems

## Slide 30
Cambering along the side of the drum
Transverse cracks behind drum
Asphalt Compaction Problems

## Slide 31
Longitudinal cracks
Asphalt Compaction Problems

## Slide 32: Questions?